Component Technical Specification (CTS)

Metallic Reinforcements, Brackets and Welded / Bonded Assemblies including Door-In-White

Prepared by:

Mike Buckland

(Technical Specialist: DIW Below Belt)

GM Confidential

Program Name:

2028 T1XX-2 SUV

Date: 06/28/2024

Template Approvals:

Version 2.0

| Region | Name of Approved | Date Approval Rec’d |
| --- | --- | --- |
| LAAM |  |  |
| GMNA |  |  |
| GMDAT |  |  |
| PATAC |  |  |
| GSSLT Leader |  |  |

Table of Contents

1	INTRODUCTION	5

1.1	Scope of Document	5

1.2	Mission/Theme	5

1.3	Classification	5

2	APPLICABLE DOCUMENTS	5

2.1	External Standards/Specifications	5

2.2	GM Standards/Specifications	5

2.3	Additional References	6

3	FUNCTIONAL REQUIREMENTS	6

3.1	System/Subsystem/Component/Part Definition	6

Conformance to the requirements contained in this section will be verified throughout regularly scheduled full vehicle, subsystem, and component durability testing.	6

3.1.1	Component Definition	6

3.1.2	Appearance	6

3.1.3	Content	6

3.1.3.1	Physical Content	6

3.1.3.2	Functional Content	6

3.1.3.2.1	Attachment Interfaces: The integral nut/studs (if present) provide the ability to attach components to any interfacing components/panels/assemblies.	6

3.1.3.2.2	Location: The part/assembly may provide the ability to locate the reinforced panel via locating holes, weld nut hole centers, shoulder features on weld studs or formed surfaces.	6

3.1.4	Ambient Environment	6

3.1.5	Interfaces	6

3.1.6	Usage Definition	6

3.2	Product Characteristics	6

3.2.1	Performance Requirements	6

3.2.1.1	Integral Nut / Stud Attachment / Structural Integrity.	6

3.2.1.2	Metal Joining Performance	7

3.2.1.2.1	Resistance Spot Welds	7

3.2.1.2.2	Arc Welds	7

3.2.1.2.3	Laser Welds	7

3.2.1.2.4	Mechanical Clinches	7

3.2.1.3	Adhesive Joining Performance	7

3.2.1.3.1	Structural Adhesive Performance for Metallic Assemblies	7

3.2.1.3.2	Hem Flange Adhesive Performance for Metallic Assemblies	7

3.2.1.3.3	Anti-Flutter Mastic Performance	7

3.2.1.3.4	Pre-formed Expandable Sealer Performance	7

3.2.1.4	Corrosion Resistance	7

3.2.1.5	Component Drop	7

3.2.2	Physical Characteristics	8

3.2.2.1	Dimensions and Capacity	8

3.2.2.2	Mass Properties	8

3.2.3	Reliability & Durability	8

3.2.3.1	Durability	8

3.2.3.2	Class 1- and 2-type problems	8

3.2.3.3	Reliability Requirements	8

3.2.4	Serviceability	8

3.2.5	User-System / Subsystem / Component / Part Interface	8

3.3	Design and Construction	8

3.3.1	Materials, Processes and Parts Selection Guidelines	8

3.3.1.1	Materials	8

3.3.1.2	Additional Coatings	8

3.3.1.3	Processes Guidelines	8

3.3.1.4	Parts Guidelines	9

3.3.2	Design Guidelines and Constraints	9

3.3.3	Identification and Marking	9

3.3.3.1	Part Identification	9

3.3.3.2	Required Labels and Markings	9

3.3.3.3	Other Marks and Labels	9

3.3.4	Workmanship	9

3.3.5	Interchangeability	9

3.4	Documentation	9

3.5	Support of System / Subsystem / Component / Part after Sale	9

3.6	System/Subsystem/Component/Part Operator Training	9

3.7	System/Subsystem/Component/Part Characteristics	9

3.7.1	System/Subsystem/Component/Part Definition	9

4	VALIDATION	9

4.1	General	9

4.2	Validation Cross Reference Index (VCRI)	10

4.3	Supporting Paragraphs	10

4.3.1	Pre-Production Builds	10

5	Provisions for Shipping	10

6	Notes	10

6.1	Glossary	10

6.2	Acronyms, Abbreviations and Symbols	10

7	Additional Paragraphs	11

7.1	11

7.2	11

8	Coding System	11

9	Release and Revisions	11

9.1	Release	11

9.2	Revisions	11

# INTRODUCTION

## Scope of Document

This specification establishes the requirements for metallic reinforcements, brackets, welded / bonded assemblies and plates, (all with or without integral threaded fasteners).

## Mission/Theme

Not Applicable.

## Classification

This document defines component specifications only.

Note: In the event of a conflict between the text of this specification and the documents cited herein, the text of this specification takes precedence.

Note: Nothing in this specification supersedes applicable laws unless a specific government exemption has been obtained.

# APPLICABLE DOCUMENTS

Note: Only the latest approved standards are applicable unless otherwise specified.

## External Standards/Specifications

| None |  |  |
| --- | --- | --- |

## GM Standards/Specifications

| GMW17679 | Metal Surface Preparation |
| --- | --- |
| GMW16215 | Weld Acceptance Criteria and Repair Procedures: Resistance Projection Welded Steel Nuts, Studs, Cages, and Other Parts with Solid Coined Projections |
| GMW14085 | Acceptance Criteria and Repair Procedures: Mechanical Clinch Joining |
| GMW14056 | Weld Acceptance Criteria and Repair Procedures: Drawn-Arc Welded Automotive Studs, Nuts, and Brackets |
| GMW14058 | Weld Acceptance Criteria and Repair Methods: Arc Welded and Arc Brazed Joints |
| GMW15425 | Weld Acceptance Criteria and Repair Procedures for Laser Fillet Welds in Lap Joints - Steel |
| GMW17330 | Laser Lap Welding Acceptance and Repair Procedure |
| GMW14057 | Weld Acceptance Criteria and Repair Methods: Resistance Spot Welds - Steel |
| GMW16967 | Aluminum Resistance Spot Welding |
| GMW16772 | Laser Welded Blanks Fabricated from Sheet Steel |
| GMW15625 | Adhesive Application Approval Requirements |
| GMW16537 | Metal Bonding Structural Adhesive Acceptance Criteria and Repair Procedures |
| GMW18077 | Body Structure Adhesive Material Requirements |
| GMW17153 | Hem Flange Adhesive Acceptance Criteria and Repair Methods |
| GMW14874 | Anti-flutter Adhesive/Sealer (Body in White) Performance Requirements |
| GMW18076 | Anti-Flutter Adhesive (Body in White) Material Requirements |
| GMW16150 | Pre-formed Expandable Sealer Performance Requirements |
| GMW18374 | Extrude-In-Place (XIP) Anti-flutter/Sealer Materials Specification |
| GMW15921 | Adhesion Requirements for Bonding Exterior Fiber Reinforced and Non-Fiber |
| GMW16185 | Adhesive Performance Requirements of Bonded FRP and Non-FRP Assemblies |
| GMW16569 | Paint / Glass Bonding Compatibility |

## Additional References

PPQP

PPAP

# FUNCTIONAL REQUIREMENTS

## System/Subsystem/Component/Part Definition

### Conformance to the requirements contained in this section will be verified throughout regularly scheduled full vehicle, subsystem, and component durability testing.

### Component Definition

The Metallic Reinforcements, Brackets and Welded / Bonded Assemblies may be used for a variety of purposes that may include adding strength or stiffness to a subsystem or providing an interface to attach another component.

### Appearance

Visible manufacturing features (not represented in the math model) shall be minimized. Boundary samples (with descriptive dimensions) for expected manufacturing features must be provided as part of the quote package. Agreed upon dimensions will be included in the drawing notes/file log for final UG math models. Requirements for panel surface quality and jewel radii can be found in SOR Appendix B

### Content

#### Physical Content

The part/assembly content is defined in the accompanying math data file. It may contain any/all the following: Stamped Panels/brackets/plates, Fasteners and/or weldments.

#### Functional Content

##### Attachment Interfaces: The integral nut/studs (if present) provide the ability to attach components to any interfacing components/panels/assemblies.

##### Location: The part/assembly may provide the ability to locate the reinforced panel via locating holes, weld nut hole centers, shoulder features on weld studs or formed surfaces.

### Ambient Environment

Operation Environmental conditions for all usage at the subsystem and vehicle level are as follows:

The welded / bonded assembly shall not discolor or distort under normal operating temperatures (-40C to 80C).

### Interfaces

Not applicable for a component specification.

### Usage Definition

The customer usage data given in this document is detailed in the durability sections of the CTS

## Product Characteristics

### Performance Requirements

#### Integral Nut / Stud Attachment / Structural Integrity.

The mating surface (of the part to which the nut/stud is attached) must be free of surface distortions from the welding or clinching/piercing process.

##### Projection Weld Nuts / Studs

Weld nuts/studs present in the part design shall meet the requirements of GMW16215 (projection type).

##### Drawn Arc Type - Weld Nuts / Studs

Weld nuts/studs present in the part design shall meet the requirements of GMW14056 (drawn arc type).

##### Self-Piercing / Clinch Nuts

Any self-piercing/clinch nuts shall meet the requirements of GMW14085.

#### Metal Joining Performance

Please visit the CCRW website (http://supplier.body.gm.com/crw/production/index.cfm) and follow the links ‘Global Standards, Specifications and Procedures’ and then ‘Global Welding Standards’ for the most updated standards.

##### Resistance Spot Welds

Any resistance spot welding present in the design shall meet the requirements of GMW14057 & GMW16967.

##### Arc Welds

Any arc welds present in the design shall meet the requirements of GMW14056 and GMW14058.

##### Laser Welds

Any laser welds present in the design shall meet the requirements of GMW15425 and GMW17330.

##### Mechanical Clinches

Any mechanical clinches present in the design must meet the requirement of GMW14085.

#### Adhesive Joining Performance

##### Structural Adhesive Performance for Metallic Assemblies

Any structural adhesive joints present in the design of a metallic assembly shall meet the requirements of GMW16537 & GMW18077.

##### Hem Flange Adhesive Performance for Metallic Assemblies

Any hem flange adhesive joints present in the design of a metallic assembly shall meet the requirements of GMW17153.

##### Anti-Flutter Mastic Performance

Any anti-flutter mastic joints present in the design shall meet the requirements of GMW14874 & GMW18076

##### Pre-formed Expandable Sealer Performance

Any preformed (non-pumpable) sealer materials, formed into parts (e.g. adhesive tapes, baffles, etc.) shall meet the requirements of GMW16150.

##### Structural Adhesive Performance for Composite Assemblies

Composite doors with bonding shall meet the requirements of GMW15921 (Adhesion Requirements for Bonding Exterior Fiber Reinforced and Non-Fiber), and GMW16185 (Adhesive Performance Requirements of Bonded FRP and Non-FRP Assemblies)

##### Low Modulus Adhesive Performance for Composites Assemblies

Composite doors with low modulus adhesive shall meet the requirements of GMW16569 (Paint / Glass Bonding Compatibility)

#### Corrosion Resistance

The parts/assemblies shall have no visible white corrosion or red rust at the time of delivery to the GM assembly plant. They should meet metal surface requirements of GMW17679. Additional ELPO coatings may be prescribed to inhibit galvanic corrosion when a steel reinforcement is attached to an aluminum panel (refer to Appendix F10 for coating specifications).

### Physical Characteristics

#### Dimensions and Capacity

All dimensions of the parts/assemblies shall conform to math data and GD&T requirements provided by General Motors.  See Appendix B.

#### Mass Properties

Not applicable – must conform to math data.

### Reliability & Durability

#### Durability

Not applicable

#### Class 1- and 2-type problems

Not applicable.

#### Reliability Requirements

Not applicable

### Serviceability

Not Applicable.

### User-System / Subsystem / Component / Part Interface

Not Applicable.

## Design and Construction

### Materials, Processes and Parts Selection Guidelines

#### Materials

See Appendix F10 of the SOR for material requirements of the parts/assemblies.

#### Additional Coatings

See Appendix F10 for additional coatings that may be required.

Note: Reinforcements that are joined to an aluminum hood or reinforcement require additional E-Coating to prevent galvanic corrosion.

#### Processes Guidelines

Laser Cutting Process Requirement:

Laser cutting techniques shall employ inert gas shielding that produce clean, oxide free surfaces in order to meet GM Paint performance and corrosion standards.  American Welding Society Standard C7.2M 2010 “Recommended Practices for Laser Beam Welding, Cutting and Allied Process” provides some general guidelines for laser cutting.  Nitrogen shielding or assist gas is required for clean laser cutting Steel, Galvanized Steel, Aluminum and Stainless steel.

#### Parts Guidelines

Not Applicable.

### Design Guidelines and Constraints

Not Applicable.

### Identification and Marking

#### Part Identification

#### Required Labels and Markings

Requirements for part marking and labels to be found in SOR Appendix B.

#### Other Marks and Labels

No supplier labels or trademarks marks are allowed on the part.

### Workmanship

All parts must be free of tool marks, nicks and burrs, sharp edges or flashing.

### Interchangeability

Not Applicable.

## Documentation

Documentation of evidence of compliance with the requirements stated herein shall be provided upon request by GM. Additionally, the lack of specific documentation requirements in this document does not negate the documentation requirements stated in the SOR (e.g. PPAP etc.).

## Support of System / Subsystem / Component / Part after Sale

Not Applicable – Per SOR.

## System/Subsystem/Component/Part Operator Training

Not Applicable.

## System/Subsystem/Component/Part Characteristics

Not Applicable.

### System/Subsystem/Component/Part Definition

Not Applicable.

# VALIDATION

## General

Validation is the process of confirming, through analyses, demonstrations, inspections, and tests, that the product meets its requirements. The subsystem will be validated to the requirements herein in accordance with GM Test Procedures. Component suppliers will work with the Vehicle Engineering Center Reliability & Test Activity to establish instrumentation, procedures, and methods to use in performing subsystem validation, and certifying results.

## Validation Cross Reference Index (VCRI)

The VCRI is a matrix that maps the performance requirements from this technical specification to their respective evaluation procedures. The VCRI resides, as a portion or section of, the Program Specific ADVP&R document that is provided by the responsible GM Validation Engineer as SOR Appendix G3. Reference Appendix G3 (CG2953) for up to date requirements.

## Supporting Paragraphs

### Pre-Production Builds

All pre-production parts shall be design validated before GM agreement to build IVER date. All parts/assemblies shall be constructed with production tools and processes and be PPQP approved through supplier quality. The Process Failure Mode Analysis (PFMA) and Design Failure Mode Analysis (DFMA) shall be approved by GM Engineering. Parts will be used by GM and the supplier to validate the product design and manufacturing processes. Any part failure will require immediate root cause analysis by supplier.

There are multiple tests that will be performed by GM at the sub-system (closure level) and vehicle level that will include door assemblies. Issues that occur during these tests related to doors will result in PRTS issues that need to be resolved by the supplier. This is not an all-inclusive list, please see your validation engineer for the latest requirements and procedures

### Vehicle Level Testing (See program specific Subsystem technical Specifications (SSTS):

Vehicle Durability				Per VTS

Squeaks, Rattles, Noise, & Vibration		GMW14011

Exterior Freeze Performance			GMW15576

Car Wash					GMW14528

CO Intrusion					GMW14824

Dust Intrusion					GMW14527

Body Leakage					GMW15470

Water Management				GMW15789

Door Closing Sound Quality			GMW14055/14233

Corrosion					GMW15272

### Side Closures Testing:

Door Slam Durability				GMW15094

Door Check Durability				GMW15093

Side Door Freeze Performance			GMW15085

# Provisions for Shipping

Parts must be supplied to the GM facility in an appropriate container such that damage, entanglement or any condition that affects performance or processing is prevented.

# Notes

## Glossary

## Acronyms, Abbreviations and Symbols

ADVP&R:  Analysis. Development. Validation. Plan & Report

CTS:  Component Technical Specification

GMNA:	General Motors North America

PPAP:	Production Part Approval Process

PPQP:	Production Process Quality Process

PRTS:  Problem Resolution Tracking System

SOR: Statement of Requirements

VCRI:  Validation Cross Reference Index

# Additional Paragraphs

## Rules and Regulations for Material Specifications

All materials supplied to this specification must comply with the requirements of GMW3001, Rules and Regulations for Material Specifications.

## Restricted and Reportable Substances for Parts

All materials supplied to this specification must comply with the requirements of GMW3059, Restricted and Reportable Substances for Parts.

# Coding System

This general specification shall be referenced in other documents, drawings, VTS, SSTS, etc. as follows:

Component Technical Specification (CTS) Torque Rods – Build-to-Print

# Release and Revisions

## Release

This general specification originated in Sep. 2, 2010.

## Revisions

This Change Log lists all approved changes implemented in this document since the last published version.

| Paragraph Affected | Description of Change | Approver / Approval Date | Requester | Changes Included in Version |
| --- | --- | --- | --- | --- |
| All | Initial Release (largely extracted from GMN11241) | 2-Sep-10 | Peter Snede |  |
| 4.2 | Updated VCRI for correctness | 3-Sep-10 | Peter Snede |  |
| 3.1.6 | Updated target life verbiage | 4-Aug-15 | Gary Murawa |  |
| 4.1 - 4.3 | Updated Validation section to reference Appendix G3 for ADVP&R | 6-Apr-17 | Gary Murawa |  |
| All | -Changed GM Logo -Owner transferred from Peter Snede to M. Buckland. -Updated material spec table (2.2) -Replaced GP-11 with PPQP -Updated all instances of “steel reinforcements…welded assemblies” with “metallic reinforcements…welded/bonded assemblies” - Deleted Section 3.2.1.5 Component drop - Updated performance requirements (3.2.1) - Updated process guidelines (3.3.1.3) - Updated validation section (4.1, 4.2, 4.3) - Added undefined acronyms to list - Updated some formatting | 31Aug21 | Michael Buckland |  |